LODE · Custom Session SOP JEOL JSM-IT800 SEM-EDS — fracture surface morphology Booking VEIN-0019 · Generated 2026-05-25 17:24

INSTRUMENT JEOL JSM-IT800 SEM-EDS; RESEARCHER Dr. Priya Anand; RESEARCH GROUP Trace Geochemistry; MATERIAL martensitic steel. SAMPLE 5mm × 5mm; SESSION Tue, May 26 · 09:00–12:00 EDT; PREP STARTS Tue, May 26 · 07:00; FIT SCORE 92/100 (A).

CUSTOMIZED SAMPLE-SPECIFIC NOTES This SOP is customized for Dr. Priya Anand's fracture surface morphology on martensitic steel. Sample prep (90 min) included before session. Cited RAG sources are listed at the end of this document.

RECOMMENDED OPERATING PARAMETERS

| Parameter | Recommended value (with citation) |
| --- | --- |
| Accelerating voltage | 10–20 kV [Historical Run Log Run #2] |
| Coating | Carbon, 5–10 nm [Historical Run Log Run #2] |
| Working distance | 10 mm [Historical Run Log Run #2] |
| Spot size | Auto (medium) |

PRE-SESSION CHECKLIST  (CUSTOMIZED TO SAMPLE)

☐  Carbon coat 5mm × 5mm at Station 2B (~90 min)  [Historical Run Log Run #2]

☐  Confirm safety training for JEOL JSM-IT800 SEM-EDS is current

☐  Arrive by 07:00 for warm-up and prep

☐  Review SDS for martensitic steel and lab EH&S guidelines  [Historical Run Log Run #8]

☐  Bring USB drive labelled with research group

STEP-BY-STEP PROCEDURE

1. Warm-up — Power on the instrument and complete its warm-up cycle (~30 min).  [Historical Run Log Run #8]

2. Load sample — Mount martensitic steel (5mm × 5mm). Verify surface level and stage clearance.  [Historical Run Log Run #2]

3. Configure — Apply parameters above for fracture surface morphology.  [Historical Run Log Run #2]

4. Acquire data — Run the planned scan / image series for fracture surface morphology. Monitor for saturation or charging.

5. Export — Save raw files to lab server under your group folder.

6. Shutdown — Follow instrument-specific shutdown checklist in the lab binder.

POST-RUN CHECKLIST

☐  Submit LODE post-run report with actual parameters + quality rating

☐  Log instrument hours and any anomalies in the maintenance log

☐  Backup raw data to research group share within 24 hours

☐  Notify lab manager of any DET-SAT, VAC-LOW, or charging issues

SAFETY NOTES

•  Handle martensitic steel per Mines EH&S guidelines.  [Historical Run Log Run #8]

•  PPE: safety glasses (and gloves when handling powders).

•  Hazardous materials flagged — coordinate with EH&S before session.

RAG REFERENCES

This SOP was generated by LODE's authoring agent grounded in the following lab knowledge sources (manuals, lab SOPs, maintenance logs).

[1] Historical Run Log — Run #2

[2] Historical Run Log — Run #8

[3] Historical Run Log — Run #6

[4] Historical Run Log — Run #7

[5] Historical Run Log — Run #9

[6] Historical Run Log — Run #5

[7] JEOL JSM-IT800 EDS/EBSD Attachment Guide — 6.1 EDS vs EBSD Selection (p.112)

[8] jeol-sem — jeol-sem

Fit rationale: SEM with EDS is optimal for fracture surface chemistry mapping at the sample scale described. [Source: JEOL JSM-IT800 Manual, Section 3.2, p.42] Carbon coating required before imaging.